An.1: Material flow chart

An.2: Energetic flow chart

An.3: Water flow chart

An.5a: Batch process scheme.

| Department | discontinuous dyeing |
| --- | --- |
| Fabric | 100% PES |
| Process | dyeing with disperse dyestuff (all colour shades) |
| Equipment | jet |
| Item | J7-8-12-13 |
| Run time (h) | 6.5 |
| Number of run/yr |  |
| Processed fabric (kg/yr) |  |
| Processed fabric per run (kg) | 145 |

data given of both medium shade and dark shade:

in practise: 3 types of dyeing can be done: light, medium or dark, each followed by a series of aftertreatments

| Water: 1400 l disperse dyestuff: 0.1-3.5% levelling agent: 1-1.5% acetic acid/sodiumacetate: 5 ml/kg formic acid Steam | dyeing (medium shade) | Discharge type (l): 1400 l – uptake by fabric T [°C]= 73 pH [-]=4.5 Conductivity [mS/cm]=2.18 COD [mg/l]=4870 BOD [mg/l]=1660 SST [mg/l]=30 |
| --- | --- | --- |
|  | OR |
| Water:1400 l disperse dyestuff: 0.1-3.5% levelling agent: 1-1.5% acetic acid/sodiumacetate: 5 ml/kg formic acid Steam | dyeing (dark shade) | Discharge type (l): 1400 l – uptake by fabric T [°C]=70 pH [-]=4.6 Conductivity [mS/cm]=3.06 COD [mg/l]=9380 BOD [mg/l]=1590 SST [mg/l]=21 |
| Water: 1400 l hydrosulfite: 40 g/kg NaOH: 30 ml/kg | reduction cleaning (only middle and dark shades) values for dark shade (2.5% dyestuff) | Discharge type (l):1 400 l T [°C]=76 pH [-]=11.48 Conductivity [mS/cm]=9.37 COD [mg/l]=7400 SST [mg/l]=45 |
| Water: 1400 l | rinsing (values for dark shade, 2.5% dyestuff) | Discharge type (l): 1 400 l T [°C]=40 pH [-]=9.71 Conductivity [mS/cm]=1.164 COD [mg/l]=718 SST [mg/l]=11 |
| Water: 1400 l | rinsing (values for dark shade, 2.5% dyestuff) | Discharge type (l): 1 400 l T [°C]=30 pH [-]=9.5 Conductivity [mS/cm]=1.022 COD [mg/l]=607 SST [mg/l]=35 |
|  | OR |
| Water: 1400 l | rinsing (values for light shade, 0.058% dyestuff) | Discharge type (l): 1 400 l T [°C]=35 pH [-]=7.5 Conductivity [mS/cm]=0.708 COD [mg/l]=678 SST [mg/l]=64 |

(*):refer to An.9

An.5a: Batch process scheme.

| Department | discontinuous dyeing |
| --- | --- |
| Fabric | 100% PA or dyeing the PA in a PA/CO mixture |
| Process | dyeing with acid (80%) or metal-complex (20%) dyestuff (all colour shades) preference is always given to acid dyestuff, if the required colour shade is not feasible with acid dyestuff then metal-complex dyestuff are used. |
| Equipment | jet |
| Item | J2-3-4-5-6-9-10-11 |
| Run time (h) | 12 |
| Number of run/yr |  |
| Processed fabric (kg/yr) |  |
| Processed fabric per run (kg) | J2-3-11: 250 kg; J4-5-9-10: 300 kg; J6: 600 kg |

J2-3-11: volume: 2000 l,   J4-5-9-10: volume: 3000 l,     J6: volume: 6000 l

| Water acid dyestuff: 0.1-3.5% levelling agent: 1-1.5% crease-preventing agent acetic acid/sodiumacetate: 5 ml/kg Steam | acid dyeing | Discharge type (l): depending on jet: volume – uptake by fabric T [°C]=70 pH [-]=4.23 Conductivity [mS/cm]=1.99 COD [mg/l]=3890 BOD [mg/l]=588 SST [mg/l]= <20 |
| --- | --- | --- |
| Water fixation agent:20-40 g/kg | cationic fixation (only middle and dark shades) values for dark shade dyeing, 1.5% dyestuff | Discharge type (l): depending on jet T [°C]=70 pH [-]=5.65 Conductivity [mS/cm]=1.873 COD [mg/l]=6752 SST [mg/l]=20 |
| Water | rinsing (values for dark shade, 1.5% dyestuff) | Discharge type (l): depending on jet T [°C]=39 pH [-]=7.71 Conductivity [mS/cm]=0.816 COD [mg/l]=389 SST [mg/l]=29 |
| Water | rinsing (values for dark shade, 1.5% dyestuff) | Discharge type (l): depending on jet T [°C]=35 pH [-]=8.06 Conductivity [mS/cm]=0.979 COD [mg/l]=69 SST [mg/l]=6 |
|  | OR |
| Water | rinsing (values for light shade, 0.25% dyestuff) | Discharge type (l): depending on jet T [°C]=36 pH [-]=7.8 Conductivity [mS/cm]=0.785 COD [mg/l]=579 SST [mg/l]=6 |

| Water metal-complex dyestuff: 0.1-3.5% levelling agent: 1-1.5% crease-preventing agent acetic acid/sodiumacetate: 5 ml/kg Steam | metal-complex dyeing | Discharge type (l): depending on jet: volume – uptake by fabric T [°C]=72 pH [-]=4.7 Conductivity [mS/cm]=4.22 COD [mg/l]=5400 BOD [mg/l]=1040 SST [mg/l]= 72 |
| --- | --- | --- |
| Water fixation agent:20-40 g/kg | cationic fixation (only middle and dark shades) values for dark shade, 2% dyestuff | Discharge type (l): depending on jet T [°C]=70 pH [-]=4.6 Conductivity [mS/cm]=3.32 COD [mg/l]=11750 SST [mg/l]=86 |
| Water | rinsing (values for dark shade, 2% dyestuff) | Discharge type (l): depending on jet T [°C]=35 pH [-]=7.19 Conductivity [mS/cm]=0.923 COD [mg/l]=923 SST [mg/l]=29 |
| Water | rinsing (values for dark shade, 2% dyestuff) | Discharge type (l): depending on jet T [°C]=30 pH [-]=7.5 Conductivity [mS/cm]=0.828 COD [mg/l]=709 SST [mg/l]=32 |

An.5.b: Continuous process scheme

| Department | continuous dyeing |
| --- | --- |
| Fabric | PES and PA |
| Process | desizing of PES and PA |
| Equipment | desizing line |
| Item | DL1 |
| Operating | continuous |
| Number of cycles/yr |  |
| Cycle time |  |
| Processed fabric (kg/yr) | 2 217 600 |
| Processed fabric per hour (kg/h) | 412 |

| water (l/min): 8 detergent water | desizing (2 compartments) rinsing (2 compartments) fixation/drying (depending on quality requirements) | data on compartment 1 (after desizing of PES): T [°C]=90 pH [-]=8.56 Conductivity [mS/cm]=2.08 COD [mg/l]=33400 BOD [mg/l]=2740 SST [mg/l]= 110 |
| --- | --- | --- |

(*):refer to An.9

An.5.b: Continuous process scheme

| Department | continuous dyeing |
| --- | --- |
| Fabric | CO/PES or CO/PA |
| Process | desizing of PES and PA in mixtures + bleaching of cotton in mixtures |
| Equipment | bleaching line |
| Item | BL1 |
| Operating | continuous |
| Number of cycles/yr |  |
| Cycle time |  |
| Processed fabric (kg/yr) | 3 449 600 |
| Processed fabric per hour (kg/h) | 642 |

| Water detergent soda water H2O2 NaOH detergent stabilising agent sequestering agent MgCl steam water | desizing of PES or PA (3 compartments) bleaching (1 compartment) steamer rinsing (2 compartments) drying on drying drum | data of compartment 1: T [°C]=87 pH [-]=11.88 Conductivity [mS/cm]=93.1 COD [mg/l]=26200 BOD [mg/l]=1300 SST [mg/l]= 181 data of compartment 1: T [°C]=93 pH [-]=9.85 Conductivity mS/cm]=1.05 COD [mg/l]=322 BOD [mg/l]=<6 SST [mg/l]=<20 |
| --- | --- | --- |

(*):refer to An.9

An.5.b: Continuous process scheme

| Department | continuous dyeing |
| --- | --- |
| Fabric | PES/CO |
| Process | dyeing with disperse (PES) and vat (CO) dyestuff |
| Equipment | thermosol and pad steam |
| Item | TH1-2 (data given per thermosol) + PS1 |
| Operating | continuous |
| Number of cycles/yr | 3730 |
| Cycle time | 30-45 min |
| Processed fabric (kg/yr) | 1 232 000 |
| Processed fabric per hour (kg/h) | 460-660 |

| Water (only for preparation of dyebath and rinsing of the machinery) disperse dyestuff vat dyestuff anti-migration agents wetting agent acetic acid: 5 ml/kg steam, dry air or fixation agents (depending on the desired quality) all PES/CO is rinsed on the pad-steam water ( 80 l/min). | dyeing fixation rinsing | data of a medium shade: rest of padder liquid (+ rinsing liquid) T [°C]=18 pH [-]=7 Conductivity [mS/cm]=0.935 COD [mg/l]=1530 BOD [mg/l]=62 SST [mg/l]= 33 data of first rinsing compartment (dosage of H2O2 and remainder of dyestuff and reduction agents) Discharge type (l/min): 80 T [°C]=20 pH [-]=12.02 Conductivity mS/cm]=7.08 COD [mg/l]=2020 BOD [mg/l]=164 SST [mg/l]=<20 |
| --- | --- | --- |

(*):refer to An.9

An.5.b: Continuous process scheme

| Department | continuous dyeing |
| --- | --- |
| Fabric | PES |
| Process | dyeing with disperse (PES) dyestuff |
| Equipment | thermosol |
| Item | TH3 |
| Operating | continuous |
| Number of cycles/yr | 1860 |
| Cycle time (h) | 2-3 h |
| Processed fabric (kg/yr) | 1 120 000 |
| Processed fabric per hour (kg/h) | 210-300 |

| Water (only for preparation of dyebath and rinsing of the machinery) disperse dyestuff anti-migration agents wetting agent acetic acid: 5 ml/kg dry air the rinsing is done on the thermosol water ( 50 l/min). | dyeing fixation rinsing of light shade (1.29 g/l dyestuff dosed in padder) OR rinsing of dark shade (20.28 g/l dyestuff dosed in padder) | data of a dark shade: rest of padder liquid (+ rinsing liquid) T [°C]=20 pH [-]=7 Conductivity [mS/cm]=1.72 COD [mg/l]=2910 BOD [mg/l]=249 SST [mg/l]= 65 Discharge type (l/min):50 discharge point 1: T [°C]=40 pH [-]=11.5 Conductivity [mS/cm]=1.972 COD [mg/l]=567 SST [mg/l]=11 discharge point 2: T [°C]=30 pH [-]=4 Conductivity [mS/cm]=0.72 COD [mg/l]=4706 SST [mg/l]=2 Discharge type (l/min):50 discharge point 1: T [°C]=42 pH [-]=11 Conductivity [mS/cm]=2.05 COD [mg/l]=915 SST [mg/l]=7 discharge point 2: T [°C]=31 pH [-]=4 Conductivity [mS/cm]=0.715 COD [mg/l]=1859 SST [mg/l]=2 |
| --- | --- | --- |

An.5.b: Continuous process scheme

| Department | continuous dyeing |
| --- | --- |
| Fabric | CO |
| Process | dyeing with reactive dyestuff |
| Equipment | cold pad-batch and pad-steam |
| Item | PB1 + PS1 |
| Operating | semi-continuous |
| Number of cycles/yr | 2980 |
| Cycle time | 25 min |
| Processed fabric (kg/yr) | 1 254 400 |
| Processed fabric per hour (kg/h) | 1000 |

| Water (only for preparation of dyebath and rinsing of the machinery) reactive dyestuff wetting agent sodiumsilicate NaOH on the pad-steam water ( 80 l/min). | dyeing (padding the dyestuff (dissolved in a cold bath) on the fabric in the PB1) dwelling the padded rolls to let the reactive dyestuff react with the fabric rinsing | data of a dark shade: rest of padder liquid (+ rinsing liquid) T [°C]=20 pH [-]=12 Conductivity [mS/cm]=22.9 COD [mg/l]=2180 BOD [mg/l]=<12 SST [mg/l]= 33 data of first rinsing compartment (remainder of dyestuff and auxiliaries in dyebath) Discharge type (l/min):80 T [°C]=20 pH [-]=9.67 Conductivity [mS/cm]=1.6 COD [mg/l]=119 BOD [mg/l]=7 SST [mg/l]= <20 |
| --- | --- | --- |

An.5.b: Continuous process scheme

| Department | continuous dyeing |
| --- | --- |
| Fabric | PA/CO |
| Process | dyeing with acid (PA) and reactive (CO) dyestuff |
| Equipment | pad-roll and pad-steam |
| Item | PR1 + PS1 |
| Operating | semi-continuous |
| Number of cycles/yr | 890 |
| Cycle time | 80 min |
| Processed fabric (kg/yr) | 537 600 |
| Processed fabric per hour (kg/h) | 450 |

| Water (only for preparation of dyebath and rinsing of the machinery) acid dyestuff reactive dyestuff wetting agent reserving agent (to prevent the PA to get partially coloured by the reactive dyestuff): 9 g/kg acetic acid buffer: 5 ml/kg on the pad-steam water (80 l/min) | dyeing (padding the dyestuff on the fabric in the PR1) fixation of the dyestuff during rotating storage of the padded rolls (rolls are heated with steam while rotating) rinsing of dark shade (200 g/l dyestuff dosed in padder) | data of a dark shade (29 g/l dyestuff): rest of padder liquid T [°C]=35 pH [-]=8.5 Conductivity [mS/cm]=12.16 COD [mg/l]=10590 SST [mg/l]= 303 Discharge type (l/h):80 T [°C]=28 pH [-]=11 Conductivity [mS/cm]=4.17 COD [mg/l]=16510 SST [mg/l]=10 |
| --- | --- | --- |

An.5.b: Continuous process scheme

| Department | printing |
| --- | --- |
| Fabric | PES/CO |
| Process | printing with pigments |
| Equipment | printing line |
| Item | PL1-2 (data per PL) |
| Operating | semi-continuous |
| Number of cycles/yr | 1250 |
| Cycle time | 90 min |
| Processed fabric (kg/yr) | 352 000 |
| Processed fabric per hour (kg/h) | 240 |

| Water (15 l/min for the rinsing of the rubber transporting band) pigments bonding agent (acrylate/butadieen) NH3 urea printing thickeners emulsifying agent | printing drying fixation on a stenter | data of continuous rinsing of rubber transporting band (2 sets of data, taken on 2 different production days) T [°C]=25 pH [-]=6.61 Conductivity [mS/cm]=0.708 COD [mg/l]=23 BOD [mg/l]=<3 SST [mg/l]= <20 Ntot [mg/l]= 3.4 T [°C]=25 pH [-]=7.62 Conductivity [mS/cm]=0.729 COD [mg/l]=894 BOD [mg/l]= 46 SST [mg/l]= 186 Ntot [mg/l]=46.2 cleaning of rubber transporting band on the end of a production batch: T [°C]=25 pH [-]=7.9 Conductivity [mS/cm]=0.685 COD [mg/l]=<15 BOD [mg/l]= <3 SST [mg/l]= 21 Ntot [mg/l]= 1.5 cleaning of printing screens, data of 2 different production days: T [°C]=25 pH [-]=7.55 Conductivity [mS/cm]=0.772 COD [mg/l]=2000 BOD [mg/l]=126 SST [mg/l]= 580 Ntot [mg/l]= 100 T [°C]=25 pH [-]=7.83 Conductivity [mS/cm]=0.85 COD [mg/l]=2660 BOD [mg/l]=139 SST [mg/l]= 771 Ntot [mg/l]=190 cleaning of barrels (preparation of printing pastes), data of 3 different production days: T [°C]=25 pH [-]=8.58 Conductivity [mS/cm]=2.76 COD [mg/l]=13300 BOD [mg/l]=756 Ntot [mg/l]= 540 T [°C]=25 pH [-]=7.01 Conductivity [mS/cm]=1.620 COD [mg/l]=29600 BOD [mg/l]=2210 Ntot [mg/l]= 1100 T [°C]=25 pH [-]=7.64 Conductivity [mS/cm]=1.21 COD [mg/l]=5660 BOD [mg/l]=839 Ntot [mg/l]= 670 |
| --- | --- | --- |

An.5.b: Continuous process scheme

| Department | printing |
| --- | --- |
| Fabric | PES (100%) or PA (100%) |
| Process | printing with disperse dyestuff (PES) or with acid dyestuff (PA) |
| Equipment | printing line, rinsing line |
| Item | PL1-2 (data per PL), RL1 |
| Operating | semi-continuous |
| Number of cycles/yr | 320 |
| Cycle time | 90 min |
| Processed fabric (kg/yr) | 88 000 |
| Processed fabric per hour (kg/h) | 24 |

| Water (15 l/min for the rinsing of the rubber transporting band) acid dyestuff (100% PA) disperse dyestuff (100% PES) thio-urea printing thickeners emulsifying agent development of acid dyestuff with direct steam (102°C), development of disperse dyestuff with superheated steam (180°C) water: 70 l/min | printing steaming (development of the dyestuff) rinsing fixation on a stenter | Discharge type (l) + (l/h): T [°C]=; pH [-]=; Conductivity [mS/cm]=; COD [mg/l]=. SST [mg/l]= Discharge type (l/min):70 data of PES (disperse dyestuff) T [°C]=42 pH [-]=8.52 Conductivity [mS/cm]=1.19 COD [mg/l]=1380 BOD [mg/l]=163 SST [mg/l]= 342 Ntot [mg/l]= 13.4 data of PA (acid dyestuff) T [°C]=18 pH [-]=7.85 Conductivity [mS/cm]=1.09 COD [mg/l]=322 SST [mg/l]=<20 Ntot [mg/l]= 100 |
| --- | --- | --- |